# 0671 RESENE painting

Worksection application

This branded worksection is applicable to the in situ application of coating films. It has been pre-edited for the use of RESENE PAINTS (AUSTRALIA) LIMITED. As with all NATSPEC worksections, it is the responsibility of the user to ensure it is completed appropriately for the project. The user should also check its applicability for local conditions and regulations.

Copyright of the branded worksection remains with NATSPEC.

For a complete specification a General requirements worksection should be included to cover the following:

Notice.

Inspection.

Submissions.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

Metals and prefinishes for shop-applied paint finishes to services components.

Timber finishes and treatment for preservative and water repellent treatments.

Cross referenced General and Associated Worksection(s) on which this worksection relies

The following worksections must be included, if this worksection is used, to provide a complete specification:

General requirements.

NATSPEC uses generic worksection names by default, whether or not there are branded equivalents. If you use a branded worksection instead of the corresponding generic, change cross references to it (e.g. in Associated worksections) to include the full branded name or change the branded worksection name to the same as the generic.

Since generic and branded worksections cover the same material, use only one, not both.

Documenting this and related work

You may document this and related work as follows:

Adapt the schedules in Selections to a Finishes schedule to your office documentation policy.

Specifying ESD

Refer to NATSPEC TECHreport Specifying ESD. The following may be specified here:

Low VOC Emitting paints.

## General

RESENE PAINTS (AUSTRALIA) LIMITED profile

For over 60 years, Resene have forged a reputation of excellence and quality in manufacturing products designed to meet the demanding standards of architectural and building industry professionals. The Resene product range includes paint and specialist coatings for residential and commercial buildings. To help building professionals keep abreast of new developments in our product range Resene has an innovative range of architectural services and reference materials, including technical and specification manuals, the Resene Total Colour System, samples and online information. Sophisticated tinting technology enables Resene to produce durable colour options that remain true to colour long after they have been applied. Interlinked systems for decorative and high performance coatings allow you to achieve the same spectrum of colours in a wide variety of products.

Resene is committed to protecting the environment and joined the Environmental Choice Programme in 1996. Resene’s commitment to this programme and a continuous development process reduces the risk Resene products may present to customers ensuring that safer, professional quality paint is available to everyone.

Contact Resene www.resene.com.au or call 1800 738 383 if you require information about Resene systems or need copies of product information, data sheets, colour references or the latest product updates.

### Aims

#### Responsibilities

General: Provide coating systems to substrates as follows:

Consistent in colour, gloss level, texture and dry film thickness.

Free of runs, sags, blisters, or other discontinuities.

Paint systems fully opaque.

Clear finishes at the level of transparency consistent with the product.

Fully adhered.

Resistant to environmental degradation within the manufacturer’s stated life span.

Selections: Conform to the Selections.

### Cross references

#### General

General: Conform to the General requirements worksection.

The General requirements worksection contains umbrella requirements for referenced documents, inspections, tests, samples, contractor’s submissions, proprietary items, manufacturers’ recommendations, warranties, record drawings, operation and maintenance manuals, and the like.

They need not be specified here unless you need to relocate them, for example if this is to be the specification for a package contract. In this case make sure that the interlocking contracts leave no loopholes, such as work by non-existent ‘others’, and have no overlaps.

#### Associated worksections

Associated worksections: Conform to the following:

List worksections cross referenced by this worksection. (General requirements references the Common requirements worksections. Do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

### Standards

#### Painting

General: Comply with the recommendations of those parts of AS/NZS 2311 and AS/NZS 2312 which are referenced in this worksection.

### Interpretation

#### Definitions

The Definitions subclause can be edited to suit the project or deleted if not required.

General: For the purposes of this worksection the definitions given below apply.

Additional painting definitions are provided in AS/NZS 2310.

Substrate: The surface to which the coating material is applied or is to be applied.

Background: The surface to which the undercoat is applied.

Paint: A product in liquid form, which when applied to a surface, forms a dry film having protective, decorative or other specific technical properties.

AS/NZS 2311 Table 4.1 describes paint types.

Sealer: A product used to seal substrates to prevent:

Materials from bleeding through to the surface.

Reaction of the substrate with incompatible top coats.

Undue absorption of the following coat into the substrate.

Primer, prime coat: The first coat of a painting system that is specifically designed to cope with the individual idiosyncrasies of the substrate, helps bind subsequent coats to the substrate, and which may inhibit its deterioration.

Undercoat: An intermediate coat formulated to prepare a primed surface or other prepared surface for the finishing coat.

Finish coat: The final coat of a coating system.

Gloss: The optical property of a surface, characterised by its ability to reflect light specularly.

Sheen: Gloss which is observed on an apparently matt surface at glancing angles of incidence.

Levels of gloss finish: When the specular direction is 60 degrees, a surface with the following specular gloss reading are defined as follows:

Full gloss finish between 50 and 100 gloss units.

Semi gloss between 20 and 50 gloss units.

Low gloss between 5 and 20 gloss units ( also known as low sheen).

Flat finish < 5 gloss units (also known as matt).

Opacity: The ability of a paint to obliterate the colour difference of a substrate.

Adhesion: The sum total of forces of attachment between a dry film and its substrate. See AS 1580 for tests to assess adhesion.

Gloss unit: Numerical value for the amount of specular reflection relative to that of a standard surface under the same geometric conditions.

Gloss levels can be measured on site in gloss units with a digital gloss meter.

### Inspection

#### Notice

Inspection: Give notice so that inspection may be made of the following:

Painting stages:

Completion of surface preparation.

After application of prime or seal coats.

After application of undercoat.

After application of each subsequent coat.

Clear finishing stages:

Before surface preparation of timber.

Completion of surface preparation.

After staining.

After sanding of sealer.

After application of each clear finishing coat.

Hold points, if required, should be inserted here. A project wide halt between each coat is considered impractical. Paintwork should be able to be inspected at various stages of completion in one visit, for example. If the paintwork is critical e.g. to external steelwork in a marine environment, stipulate notice required in the project specification.

The level of inspection will depend on the nature of the project and will range from full for large or complex projects, through intermittent for straightforward work, to occasional for initially establishing the standards of execution.

### Submissions

#### Clear finish coated samples

General: Submit pieces of timber or timber veneer matching the timber to be used in the works, prepared, puttied, stained, sealed and coated in accordance with the specified system, of sufficient size so that, each piece can be cut into 4 segments, marked for identification, and distributed as directed.

#### Control samples

General: Submit, on representative substrates, samples of each coating system showing surface preparation, colour, gloss level, texture, and physical properties; to the Coated samples schedule. Obtain approval in writing of the appearance before proceeding. Use the Resene Architectural Sample Box as a basis of standard where appropriate.

#### Coated samples schedule

| Substrate | Paint system | Colour | Sample size |
| --- | --- | --- | --- |
| Plasterboard | Flat waterborne: Interior | Off white | 50 x 300 mm |

Information entered in the table is an example. Edit as required.

Use this clause where appearance is the main criteria. Size and form of samples depend on the nature of the project.

#### Colour samples

Control reference: Check colours to Resene colour samples prior to application and keep the Resene colour samples on site as a control reference. Colour matches are not permitted as they will differ in appearance, durability and performance to the original selected colour over the life of the coating. Samples of Resene colours may be ordered online from https://secure.resene.co.nz/samples/samples.php?isProfessional=1 or by calling 1800 738 383.

Use the Resene Architectural Sample Box as a basis of standard where appropriate.

Use this clause where it is important that the colours used match the durability, performance and appearance of the colours selected. Colour matches supplied by other manufacturers will perform differently, particularly in the long term. For samples of Resene colours, visit www.resene.com.au or call 1800 738 383.www.resene.com.au or by calling 1800 738 383 www.resene.com.au or by calling 1800 738 383.

#### Manufacturer’s documents

Product: Refer Resene One-Line Specifications and Product Data Manual (hard copy or view online at www.resene.com.au).

It is important to ensure that all personnel on site have access to accurate, up to date technical information on the many products, materials and equipment used on a project. In most cases individual products are not used in isolation, but form part of a building process. Also a particular manufacturer’s and/or supplier’s requirements for handling, storage, preparation, installation, finishing and protection of their product can vary from what might be considered the norm. Access to technical information can help overcome this potential problem.

Safety: Submit the Resene published material safety data sheets (MSDS) showing the health and safety precautions to be taken during application. MSDS are available from www.resene.com.au or by calling 1800 738 383.

#### -Execution

General: Submit name and contact details of proposed specialist applicators.

## Products

### Paints

#### Combinations

General: Do not combine paints from different manufacturers in a paint system.

Clear timber finish systems: Provide only the combinations of putty, stain and sealer recommended by the manufacturer of the topcoats.

#### Delivery

General: Deliver paints to the site in the manufacturer’s labelled and unopened containers.

#### Tinting

General: Provide only products which are colour tinted by the manufacturer or supplier.

If tinting is by contractor, add tinters or stainers only if this is without detriment to the durability or aesthetic performance of the product.

#### Toxic ingredients

General: Comply with the requirements of Appendix I Uniform Paint Standard to the Standard for the Uniform Scheduling of Drugs and Poisons (SUSDP).

-Appendix I contains three schedules. The first lists toxic pigment components such as barium and cadmium, the second lists toxic solvents, and the third deals with lead. First Schedule paints are banned, in Appendix I, for use on roofs, furniture, fences, and gates, surfaces of non-industrial buildings and in premises used for products intended for human consumption. -Third Schedule paints are banned, in Appendix I, from use on roofs, furniture, fences, walls, gates, buildings, bridges and in premises used for products intended for human consumption. -Check for any state variations.

#### Low VOC Compliance Reference table

Low VOC emitting paints: As defined by the Green Building Council (GBC) Specifications.

The GBC parameters are only applicable to interior products or products used on interior surfaces.

>>> To earn credit points for the Green Star – Office Design v2 scheme nominate 16 g/litre for coloured low gloss latex paints.

>>> To earn credit points for the Green Star – Office Design v2 scheme nominate 75 g/litre for gloss latex paints.

Green Star Building Council (GBC) Specifications are subject to change without notice so seek latest figures.

| Green Star Office Design v2 Product Type | VOC Limits MAX g/litre | RESENE Products compared to the GBC Specification | VOC g/litre (inc tint using Resene non VOC tinters) |
| --- | --- | --- | --- |
| COMPLIANCE CRITERIA – Green Star Building Council (GBC) Specifications (obtain latest figures) |
| Exterior Flat and Low Sheen | 50 | Resene Lumbersider D34 | 35 |
| Exterior Flat and Low Sheen | 50 | Resene Waterborne Sidewalk D38a | 30 |
| Exterior Flat and Low Sheen | 50 | Resene AquaShield D601 | 7 |
| Exterior Flat and Low Sheen | 50 | Resene Sandtex Standard and Superfine D71 | 8 |
| Exterior Gloss | 75 | Resene Hi-Glo D31 | 62 |
| Exterior Latex Undercoat | 55 | Resene Quick Dry Waterborne Primer Undercoat D45 | 41 |
| Exterior Semi Gloss | 70 | Resene Sonyx 101 D30 | 59 |
| Exterior Timber Primer | 50 | Resene Quick Dry Acrylic Primer Undercoat D45 | 41 |
| Interior Flat-Ceilings | 14 | Resene Ceiling Paint D305 | 1 |
| Interior Gloss | 75 | Resene Enamacryl D309a | 63 |
| Interior Latex Undercoat | 65 | Resene Quick Dry Acrylic Primer Undercoat D45 | 41 |
| Interior Low Sheen | 16 | Resene Zylone Sheen VOC Free D302 | 0 |
| Interior Sealer | 65 | Resene Broadwall Waterborne Wallboard Sealer D403 | 0 |
| Interior Sealer | 65 | Resene Broadwall Surface Prep & Seal D807 | 27 |
| Interior Sealer | 65 | Resene Broadwall 3 in 1 D810 | 2 |
| Interior Sealer | 65 | Resene Waterborne Smooth Surface Sealer D47a | < 10 |

## Execution

### Preparation

#### Standards

General: To AS/NZS 2311 Section 3.

Protection of steelwork: To AS/NZS 2312 Section 4.

#### Order of work

Other trades: Before painting, complete the work of other trades as far as practicable within the area to be painted, except for installation of fittings, floor sanding and laying flooring materials.

Clear finishes: Complete clear timber finishes before commencing opaque paint finishes in the same area.

#### Protection

Fixtures: Remove door furniture, switch plates, light fittings and other fixtures before starting to paint, and refix in position undamaged on completion of the installation.

Adjacent surfaces: Protect adjacent finished surfaces liable to damage from painting operations.

Consider calling for masking as protection for small contracts involving existing buildings where there may not be an electrician on site.

#### ‘Wet paint’ warning

General: Place notices conspicuously and do not remove them until paint is dry.

#### Repair

General: Clean off marks, paint spots and stains progressively and restore damaged surfaces to their original condition. Touch up new damaged decorative paintwork or misses only with the paint batch used in the original application.

#### Substrate preparation

General: Prepare substrates to receive the painting systems.

Cleaning: Clean down the substrate surface. Do not cause undue damage to the substrate or damage to, or contamination of, the surroundings.

Filling: Fill cracks and holes with fillers, sealants, putties or grouting cements as appropriate for the finishing system and substrate, and sand smooth.

Clear finish: Provide filler tinted to match the substrate.

Clear timber finish systems: Prepare the surface so that its attributes will show through the clear finish without blemishes, by methods which may involve the following:

Removal of bruises.

Removal of discolourations, including staining by oil, grease and nailheads.

Bleaching where necessary to match the timber colour sample.

Puttying.

Fine sanding (last abrasive no coarser than 220 grit) to show no scratches across the grain.

### Painting

#### Painting generally

Refer to Resene One-Line Specifications and Product Data Manual data sheets and the additional requirements of this work section.

#### Standards

General: To AS/NZS 2311 Section 6.

Protection of steelwork: To AS/NZS 2312 Section 8.

#### Light levels

General: ≥400 lux.

#### Drying

General: Use a moisture meter to demonstrate that the moisture content of the substrate is at or below the recommended maximum level for the type of paint and the substrate material.

#### Paint application

General: Apply the first coat immediately after substrate preparation and before contamination of the substrate can occur. Apply subsequent coats after the manufacturer’s recommended drying period has elapsed.

#### Priming before fixing

General: Apply one coat of wood primer (2 coats to end grain) to the back of the following before fixing in position:

External fascia boards.

Timber door and window frames.

Bottoms of external doors.

Associated trims and glazing beads.

Timber board cladding.

#### Spraying

General: If the paint application is by spraying, use conventional or airless equipment which does the following:

Satisfactorily atomises the paint being applied.

Does not require the paint to be thinned beyond the maximum amount recommended by the manufacturer.

Does not introduce oil, water or other contaminants into the applied paint.

Paint with known health hazards: Not permitted on site.

#### Sanding

Clear finishes: Sand the sealer using the finest possible abrasive (no coarser than 320 grit) and avoid cutting through the colour. Take special care with round surfaces and edges.

#### Repair of galvanising

General: For galvanised surfaces which have been subsequently welded, prime the affected area.

Primer: Organic zinc rich coating, two pack, to AS/NZS 3750.9.

#### Tinting

General: Tint each coat of an opaque coating system so that each has a noticeably different tint from the preceding coat, except for top coats in systems with more than one top coat.

#### Services

General: If not embedded, paint new services and equipment including in plant rooms, except chromium, anodised aluminium, GRP, UPVC, stainless steel, non-metallic flexible materials and normally lubricated machined surfaces. Repaint proprietary items only if damaged.

## Selections

Record the selections for the project as follows:

Refer to the sub-clause for the applicable substrate and broad product group i.e. Paper faced plasterboard water based or oil based.

Select the finish required i.e. flat or low sheen.

Delete the table rows for all paint lines not applicable to the project.

Add a paint code i.e. P1, P2 if the specification selection is to be aligned to a Finishes Schedule and a Colour Schedule. Refer to colour cards, fan decks and other Resene colour tools to source the colours available for a particular paint type.

For further information refer to the Resene Spec sheet.

### Exterior painting schedules

#### Paint system schedules

Selections: Conform to the Exterior finishes schedule.

Paint system: Conform to the Exterior paint system clause identified by the Resene Specification Number.

#### Exterior finishes schedule

| Substrate | Resene Spec Number | Colour |
| --- | --- | --- |

Complete the Exterior finishes schedule as follows:

Substrate: For each application refer to the clause that describes the appropriate substrate e.g. Exterior cementitious surfaces and select the preferred finish coat type.

Resene Spec. Number: Enter the Resene ‘Spec. Number’ for the coating system associated with the finish coat description previously selected, into the Exterior finishes schedule. Activate the Word ‘Document map’ drop down from ‘View’ to facilitate faster access to the Resene product list.

Colour: Consult Resene at www.resene.com.au to select the colour. Dark colours may cause warping on unstable substrates.

Add to the table for additional substrates as required.

### Exterior paint systems

On completion of the Exterior finishes schedule delete each paint system description NOT used. The remaining paint system descriptions will instruct the builder.

Cool Colours: In exposed areas darker colours are sun traps soaking in the sun’s rays placing significant stress on the coating and the substrate. Resene has developed ‘Cool Colour’ Technology reducing heat absorption of a wide range of colours, minimising the heat buildup in the coating, substrate and heat transference inside.  Resene Cool Colours are currently available for the following products: Resene HI-Glo, Resene Sonyx 101, Resene Lumbersider, Resene X-200, Resene AquaShield, Resene Waterborne Sidewalk, Resene SpaceCote Flat, Resene Enamacryl and Resene Lustacryl.  Contact your local Resene Representative or visit www.resene.co.nz for more information.

### Exterior cementitious surfaces

Including concrete, concrete masonry, tilt slab, GRC, fibre reinforced cement boards, cement render including stucco, rough cast, EIFS

For more information: Refer to Resene website

Refer to http://www.resene.co.nz/archspec/datashts/spec1_Cementitious.pdf

Refer to http://www.resene.co.nz/archspec/datashts/spec20_Textured_Coatings.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Exterior cementitious surfaces, waterborne gloss | 1e 1.1 | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer | Resene Hi-Glo D31, waterborne gloss | Resene Hi-Glo D31, waterborne gloss 4th coat: Resene Multishield+ D54a, waterborne glaze (optional) |
| Exterior cementitious surfaces, waterborne semi-gloss | 1e 1.2 | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer; or Self priming - Resene Sonyx 101 D30, waterborne semi-gloss | Resene Sonyx 101 D30, waterborne semi-gloss | Resene Sonyx 101 D30, waterborne semi-gloss 4th coat: Resene Multishield+ D54a, waterborne glaze (optional) |
| Exterior cementitious surfaces, waterborne satin | 1e 1.3 | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer; or Self priming - Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin 4th coat: Resene Multishield+ D54a, waterborne glaze (optional) |
| Exterior cementitious surfaces, waterborne mineral flat | 20.e 1.5 SSP | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Aquapel D65; or For powdery surface - Resene Sureseal D42, solventborne sealer | Resene Aquashield D601, waterborne mineral flat | Resene Aquashield D601, waterborne mineral flat |
| Exterior cementitious surfaces, solventborne gloss | 1e 2.1 | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer | Resene Acrylic Undercoat D404, waterborne undercoat | Resene Super Gloss D32, solventborne gloss |

### Exterior timbers

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec2_Timber_Interior_Ext.pdf

http://www.resene.co.nz/archspec/datashts/spec3_Timber_Joinery.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Exterior timbers, waterborne gloss | 2e 1.1 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer | Resene Hi-Glo D31, waterborne gloss | Resene Hi-Glo D31, waterborne gloss |
| Exterior timbers, waterborne semi-gloss | 2e 1.2 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer | Resene Sonyx 101 D30, waterborne semi-gloss | Resene Sonyx 101 D30, waterborne semi-gloss |
| Exterior timbers, waterborne satin | 2e 1.3 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer; or Self priming - Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin |
| Exterior timber joinery, waterborne gloss | 3e 1.1 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer | Resene Enamacryl D309, waterborne gloss enamel | Resene Enamacryl D309, waterborne gloss enamel |
| Exterior timber joinery, waterborne semi-gloss | 3e 1.2 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer | Resene Lustacryl D310, waterborne semi-gloss enamel | Resene Lustacryl D310, waterborne semi-gloss enamel |
| Exterior timbers, solventborne gloss | 2e 2.1 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For hardboard only - Resene Sureseal D42, solventborne sealer | Resene Acrylic Undercoat D404, waterborne undercoat | Resene Super Gloss D32, solventborne gloss |

### Exterior timber, stains and clear finishes

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec2_Timber_Interior_Ext.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Exterior timbers, stains and clear finishes, waterborne stain This system is not suitable for decks | 2e 3.5 | D82 | Resene Waterborne Woodsman D57a, waterborne stain | Resene Waterborne Woodsman D57a, waterborne stain | Resene Waterborne Woodsman D57a, waterborne stain (after 3 months) |
| Exterior timbers, stains and clear finishes, solventborne flat If used on decks this system may not meet the slip resistance requirements of the building code. SRG Grit can be added to improve performance | 2e 4.5 | D82 | Resene Woodsman D57, solventborne stain | Resene Woodsman D57, solventborne stain | Resene Woodsman D57, solventborne stain |

### Exterior timber joinery

Including doors and windows. For cedar refer to 8e. For totara and matai refer to 9e.

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec2_Timber_Interior_Ext.pdf

http://www.resene.co.nz/archspec/datashts/spec3_Timber_Joinery.pdf

http://www.resene.co.nz/archspec/datashts/spec8_Cedar_Exterior.pdf

http://www.resene.co.nz/archspec/datashts/spec9_Matai_Totara.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Exterior timber joinery, waterborne gloss | 3e 1.1 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer | Resene Enamacryl D309, waterborne gloss enamel | Resene Enamacryl D309, waterborne gloss enamel |
| Exterior timber joinery, waterborne semi-gloss | 3e 1.2 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer | Resene Lustacryl D310, waterborne semi-gloss enamel | Resene Lustacryl D310, waterborne semi-gloss enamel |
| Exterior timber joinery, solventborne gloss | 3e 2.1 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer | Resene Acrylic Undercoat D404, waterborne undercoat | Resene Super Gloss D32, solventborne gloss |

### Exterior timber decks, pergolas and fences

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec4_Timber_Decks_Fences.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Exterior timber decks, pergolas and fences, waterborne satin If used on decks this system may not meet the slip resistance requirements of the building code. SRG Grit can be added to improve performance | 4e 1.3 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin |
| Exterior timber decks, non-skid finish | 4e 1.3 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | Resene Quick Dry D45, waterborne primer/undercoat | Resene Non-Skid Deck & Path D313, non-skid finish | Resene Non-Skid Deck & Path D313, non-skid finish |
| Exterior timber, pergolas and fences, waterborne stain This system is not suitable for decks | 4e 3.5 | D82 | Resene Waterborne Woodsman D57a, waterborne stain | Resene Waterborne Woodsman D57a, waterborne stain | Resene Waterborne Woodsman D57a, waterborne stain (after 3 months) |
| Exterior timber decks, pergolas and fences, solventborne stain If used on decks this system may not meet the slip resistance requirements of the building code | 4e 4.5 | D82 | Resene Woodsman D57, solventborne stain | Resene Woodsman D57, solventborne stain | Resene Woodsman D57, solventborne stain (after 3 months) |
| Exterior timber decks, pergolas and fences, solventborne stain If used on decks this system may not meet the slip resistance requirements of the building code | 4e 4.5 C | D82 | Resene Kwila Timber Stain D501, solventborne stain | Resene Kwila Timber Stain D501, solventborne stain | - |
| Exterior timber decks, pergolas and fences, solventborne stain If used on decks this system may not meet the slip resistance requirements of the building code | 4e 4.5 N | D82 | Resene Furniture and Decking Oil D503, solventborne oil | Resene Furniture and Decking Oil D503, solventborne oil | - |

### Exterior galvanized steel and Zincalume

For more information: Refer to Resene website

Refer to http://www.resene.co.nz/archspec/datashts/spec5_Steel_Galvanised_Ext.pdf

For demanding and aggressive exterior environments, refer to One-Line Specifications 22-24 or the

Resene Engineered Coating Systems Manual.

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Exterior galvanised steel and Zincalume, waterborne gloss | 5e 1.1 | D89 | For new work - Resene Galvo-Prime D402, waterborne galvanised iron primer; or For repaint - Resene Galvo One D41, solventborne galvanised iron primer 2 coats of primer strongly recommended for non-rain washed areas | Resene Hi-Glo D31, waterborne gloss | Resene Hi-Glo D31, waterborne gloss |
| Exterior galvanised steel and Zincalume, waterborne semi-gloss | 5e 1.2 | D89 | For new work - Resene Galvo-Prime D402, waterborne galvanised iron primer; or For repaint - Resene Galvo One D41, solventborne galvanised iron primer 2 coats of primer strongly recommended for non-rain washed areas | Resene Sonyx 101 D30, waterborne semi-gloss | Resene Sonyx 101 D30, waterborne semi-gloss |
| Exterior galvanised steel and Zincalume, waterborne satin | 5e 1.3 | D89 | For new work - Resene Galvo-Prime D402, waterborne galvanised iron primer; or For repaint - Resene Galvo One D41, solventborne galvanised iron primer 2 coats of primer strongly recommended for non-rain washed areas. System not suitable for roofs | Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin |
| Exterior galvanised steel and Zincalume, solventborne gloss System not suitable for roofs | 5e 2.1 | D89 | Resene Galvo One D41, solventborne galvanised iron primer | Resene Acrylic Undercoat D404, waterborne undercoat | Resene Super Gloss D32, solventborne gloss |

### Exterior cedar

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec8_Cedar_Exterior.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Exterior cedar, waterborne gloss | 8e 1.1 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | Resene Wood Primer D40, solventborne primer | Resene Quick Dry D45, waterborne primer/undercoat | Resene Hi-Glo D31, waterborne gloss 4th coat: Resene Hi-Glo D31, waterborne gloss (4th coat optional on weathered cedar) |
| Exterior cedar, waterborne semi-gloss | 8e 1.2 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | Resene Wood Primer D40, solventborne primer | Resene Quick Dry D45, waterborne primer/undercoat | Resene Sonyx 101 D30, waterborne semi-gloss 4th coat: Resene Sonyx 101 D30, waterborne semi-gloss (4th coat optional on weathered cedar) |
| Exterior cedar, waterborne satin | 8e 1.3 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | Resene Wood Primer D40, solventborne primer | Resene Quick Dry D45, waterborne primer/undercoat | Resene Lumbersider D34, waterborne satin 4th coat: Resene Lumbersider D34, waterborne satin (4th coat optional on weathered cedar) |
| Exterior cedar, solventborne gloss | 8e 2.1 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | Resene Wood Primer D40, solventborne primer | Resene Quick Dry D45, waterborne primer/undercoat | Resene Super Gloss D32, solventborne gloss 4th coat: Resene Super Gloss D32, solventborne gloss |
| Exterior cedar, waterborne stain | 8e 3.5 | D82 | Resene Waterborne Woodsman D57a, waterborne stain | Resene Waterborne Woodsman D57a, waterborne stain | Resene Waterborne Woodsman D57a, waterborne stain (after 3 months) |
| Exterior cedar, solventborne stain | 8e 4.5 | D82 | For stained finish - Resene Woodsman D57, solventborne stain | Resene Woodsman D57, solventborne stain | Resene Woodsman D57, solventborne stain (after 3 months) |
| Exterior cedar, solventborne stain, kwila timber stain colour | 8e 4.5 | D82 | Resene Kwila Timber Stain D501, solventborne stain | Resene Kwila Timber Stain D501, solventborne stain | - |

### Concrete waterproofing membranes

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec17_Waterproofing_Memb.pdf

Textured samples should be approved prior to work commencing.

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Barrier membranes, waterborne semi-gloss | 17e 1.2T | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer; or Self priming - Resene Thixalon 5 D63, waterborne semi-gloss | Resene Thixalon 5 D63, waterborne semi-gloss | Resene Thixalon 5 D63, waterborne semi-gloss 4th coat: Resene Multishield+ D54a, waterborne glaze (optional) |
| Waterproofing membranes, waterborne semi-gloss A minimum film build of 500 microns is required. | 17e 1.2F | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer; or Self priming - Resene Flexicover E D64, waterborne semi-gloss | Resene Flexicover E D64, waterborne semi-gloss | Resene Flexicover E D64, waterborne semi-gloss 4th coat: Resene Lumbersider D34, waterborne satin (optional) |
| Waterproofing membranes, waterborne low sheen | 17e 1.4 | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer; or Self priming - Resene X-200 D62, waterborne low sheen | Resene X-200 D62, waterborne low sheen | Resene X-200 D62, waterborne low sheen 4th coat: Resene Multishield+ D54a, waterborne glaze (optional) |

### Exterior metallic finishes

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec25_Special_Effects.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Exterior waterborne metallic | 25e 1.3/5 | D83 | Resene Quick Dry D45, waterborne primer/undercoat Waterborne low sheen must be applied where a barrier coat is needed. 2 full coats of Resene X-200 D62 | Resene Lumbersider D34, waterborne satin | 3rd/4th coat: Resene Enamacryl Metallic D309a, waterborne metallic 5th coat: Resene Multishield+ D54a, waterborne glaze (optional) |
| Exterior waterborne pearlescent | 25e 1.3/5 P | D83 | Resene Quick Dry D45, waterborne primer/sealer | Resene Lumbersider D34, waterborne satin | 3rd coat: Resene Lumbersider D34, waterborne satin 4th coat: Resene Pearl Shimmer D312, waterborne pearlescent 5th coat: Resene Multishield+ D54a, waterborne glaze (optional) |
| Exterior metallic finish on concrete floor, 2 pack | 25e 2.3/5 | D83 | Resene Armourcote 510 RA40, high solids epoxy | Resene Imperite IF 503 RA81, solventborne metallic | Resene Uracryl 400 Series Clear, acrylic urethane |

### Other Resene exterior systems

6e FERROUS METALS

Refer to http://www.resene.co.nz/archspec/datashts/spec6_Ferrous_Metals.pdf

7e EXTERIOR NON-FERROUS METALS

Refer to http://www.resene.co.nz/archspec/datashts/spec7_Non-Ferrous_Metals.pdf

9e EXTERIOR TOTARA AND MATAI TIMBER, STAINS AND CLEAR FINISHES

Refer to http://www.resene.co.nz/archspec/datashts/spec9_Matai_Totara.pdf

10e EXTERIOR BITUMEN, BUTYL AND EPDM RUBBERS

Refer to http://www.resene.co.nz/archspec/datashts/spec10_Bitumen_Rubbers.pdf

11e GLASS, GLAZED TILES, BAKED ENAMEL SYSTEMS

Refer to http://www.resene.co.nz/archspec/datashts/spec11_Enamel_Glass_Tiles.pdf

12e GLASS REINFORCED POLYESTER, EPOXY, PVC, ACRYLIC SHEETING, POLYSTYRENE, POLYCARBONATE

Refer to http://www.resene.co.nz/archspec/datashts/spec12_Plastic_Materials.pdf

13e BRICK AND TERRACOTTA

Refer to http://www.resene.co.nz/archspec/datashts/spec13_Brick_Terracotta.pdf

14e CLEAR FINISHES ON CLAY TILES, ABSORBENT TILES, STONE AND SLATE, DECORATIVE AGGREGATE FLOORING

Refer to http://www.resene.co.nz/archspec/datashts/spec14_Clay_Tiles_Stone.pdf

16e EXTERIOR CANVAS AND AWNINGS

Refer to http://www.resene.co.nz/archspec/datashts/spec16_Canvas_Wallpaper.pdf

18e HEAVY DUTY FLOOR COATINGS

Refer to http://www.resene.co.nz/archspec/datashts/spec18_Flooring_Specialist.pdf

19e ANTI GRAFFITI SYSTEMS

Refer to http://www.resene.co.nz/archspec/datashts/spec19_Anti-Graffiti_System.pdf

20e TEXTURED AND SPECIALIST COATINGS (INCLUDING HARDITEX)

Refer to http://www.resene.co.nz/archspec/datashts/spec20_Textured_Coatings.pdf

21e PAINT EFFECTS

Refer to http://www.resene.co.nz/archspec/datashts/spec21_Paint_Effects.pdf

### Interior painting schedules

#### Paint system schedules

Selections: Conform to the Interior finishes schedule.

Paint system: Conform to the Interior paint system clause identified by the Resene Specification Number.

#### Interior finishes schedule

| Room name | Code | Substrate | Resene Spec Number | Colour |
| --- | --- | --- | --- | --- |

Room name:

Complete the Interior finishes schedule as follows:

Room name: As appropriate for the project. Add to the table for additional rooms as required. Add a column for a room number as required.

Code: A designation code may be required to reference a Finishes Schedule to your office documentation policy. In this case the Room name and number would appear on the Finishes schedule and could be deleted here.

Substrate: For each application refer to the clause that describes the appropriate substrate e.g. Interior cementitious surfaces and select the preferred finish coat type.

Resene Spec. number: Enter the Resene ‘Spec. Number’ for the coating system associated with the finish coat description previously selected, into the Interior finishes schedule. Activate the Word ‘Document map’ drop down from ‘View’ to facilitate faster access to the Resene product list.

Colour: Consult Resene at www.resene.com.au to select the colour.

### Interior pain systems

On completion of all interior finishes delete each paint system description NOT used. The remaining paint system descriptions will instruct the builder.

# Resene interior paint systems

Interior paint systems: Supply the listed Resene systems for the following substrates.

Select the appropriate first coat by deleting those not applicable.

### Interior cementitious surfaces

For more information:

Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec1_Cementitious.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Interior cementitious surfaces, waterborne gloss | 1i 1.1 | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer | Resene Enamacryl D309, waterborne gloss | Resene Enamacryl D309, waterborne gloss |
| Interior cementitious surfaces, waterborne semi-gloss | 1i 1.2 | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer; or Self priming - Resene Lustacryl D310, waterborne semi-gloss enamel | Resene Lustacryl D310, waterborne semi-gloss enamel | Resene Lustacryl D310, waterborne semi-gloss enamel |
| Interior cementitious surfaces, waterborne satin | 1i 1.3 | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer; or Self priming - Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin |
| Interior cementitious surfaces, waterborne low sheen | 1i 1.4 ZS | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer; or Self priming - Resene Zylone Sheen or Resene Zylone Sheen VOC Free D302, waterborne low sheen | Resene Zylone Sheen or Resene Zylone Sheen VOC Free D302, waterborne low sheen | Resene Zylone Sheen or Resene Zylone Sheen VOC Free D302, waterborne low sheen |
| Interior cementitious surfaces, waterborne low sheen | 1i 1.4 SC | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer; or Self priming - Resene SpaceCote Low Sheen D311, waterborne low sheen enamel | Resene SpaceCote Low Sheen D311, waterborne low sheen enamel | Resene SpaceCote Low Sheen D311, waterborne low sheen enamel |
| Interior cementitious surfaces, waterborne flat | 1i 1.5 | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer; or Self priming - Resene Zylone 20 D37, waterborne flat | Resene Zylone 20 D37, waterborne flat | Resene Zylone 20 D37, waterborne flat |
| Interior cementitious surfaces, waterborne flat enamel | 1i 1.5 SC | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer; or Self priming - Resene SpaceCote Flat D314, waterborne flat enamel | Resene SpaceCote Flat D314, waterborne flat enamel | Resene SpaceCote Flat D314, waterborne flat enamel |
| Interior cementitious surfaces, solventborne gloss | 1i 2.1 | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer | Resene Acrylic Undercoat D404, waterborne undercoat | Resene Super Gloss D32, solventborne gloss |
| Interior cementitious surfaces, solventborne semi-gloss | 1i 2.2 | D83 For thin plaster - Resene Limelock D809, waterborne cure/seal | For sound cementitious surfaces - Resene Concrete Primer D405, waterborne primer; or For powdery surfaces - Resene Sureseal D42, solventborne sealer | Resene Lusta-Glo D33, solventborne semi-gloss | Resene Lusta-Glo D33, solventborne semi-gloss |

### Interior timber

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec2_Timber_Interior_Ext.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Interior timber, waterborne gloss | 2i 1.1 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Enamacryl D309, waterborne gloss enamel; or Resene Acrylic Undercoat D404, waterborne undercoat | Resene Enamacryl D309, waterborne gloss enamel |
| Interior timber, waterborne semi-gloss | 2i 1.2 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Lustacryl D310, waterborne semi-gloss enamel; or Resene Acrylic Undercoat D404, waterborne undercoat | Resene Lustacryl D310, waterborne semi-gloss enamel |
| Interior timber, waterborne satin | 2i 1.3 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer; or Self priming - Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin |
| Interior timber, waterborne low sheen | 2i 1.4 ZS | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer; or Self priming - Resene Zylone Sheen or Resene Zylone Sheen VOC Free D302, waterborne low sheen | Resene Zylone Sheen or Resene Zylone Sheen VOC Free D302, waterborne low sheen | Resene Zylone Sheen or Resene Zylone Sheen VOC Free D302, waterborne low sheen |
| Interior timber, waterborne satin | 2i 1.4 SC | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer; or Self priming - Resene SpaceCote Low Sheen D311, waterborne low sheen enamel | Resene SpaceCote Low Sheen D311, waterborne low sheen enamel | Resene SpaceCote Low Sheen D311, waterborne low sheen enamel |
| Interior timber, waterborne flat | 2i 1.5 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer; or Self priming - Resene Zylone 20 D37, waterborne flat | Resene Zylone 20 D37, waterborne flat | Resene Zylone 20 D37, waterborne flat |
| Interior timber, waterborne flat enamel | 2i 1.5 SC | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer; or Self priming - Resene SpaceCote Flat D314, waterborne flat enamel | Resene SpaceCote Flat D314, waterborne flat enamel | Resene SpaceCote Flat D314, waterborne flat enamel |
| Interior timber, solventborne gloss | 2i 2.1 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45,waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Acrylic Undercoat D404, waterborne undercoat | Resene Super Gloss D32, solventborne gloss |
| Interior timber, solventborne semi-gloss | 2i 2.2 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45, waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For hardboard only - Resene Sureseal D42, solventborne sealer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Lusta-Glo D33, solventborne semi-gloss; or Resene Acrylic Undercoat D404, waterborne undercoat | Resene Lusta-Glo D33, solventborne semi-gloss |

### Interior timber, stains and clear finishes

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec2_Timber_Interior_Ext.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd/4th/5th coat |
| --- | --- | --- | --- | --- | --- |
| Interior timber, stains and clear finishes, waterborne gloss | 2i 3.1 | D82 | Stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or Clear finish - Resene Waterborne Colorwood Reducing Base D50a, waterborne clear (optional) | Resene Aquaclear D59, waterborne gloss urethane | Resene Aquaclear D59, waterborne gloss urethane |
| Interior timber, stains and clear finishes, waterborne semi-gloss | 2i 3.2 | D82 | Stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or Clear finish - Resene Waterborne Colorwood Reducing Base D50a, waterborne clear (optional) | Resene Aquaclear D59, waterborne semi-gloss urethane | Resene Aquaclear D59, waterborne semi-gloss urethane |
| Interior timber, stains and clear finishes, waterborne satin | 2i 3.3 | D82 | Stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or Clear finish - Resene Waterborne Colorwood Reducing Base D50a, waterborne clear (optional) | Resene Aquaclear D59, waterborne satin urethane | Resene Aquaclear D59, waterborne satin urethane |

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd/4th coat |
| --- | --- | --- | --- | --- | --- |
| Interior timber, stains and clear finishes, solventborne gloss | 2i 4.1 | D82 | Stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or Clear finish - Resene Waterborne Colorwood Reducing Base D50a, waterborne clear (optional) | Resene Poly-Flat D52, solventborne flat clear; or For particleboard and fibre board - Resene Aquaclear D59, waterborne urethane | Resene Poly-Gloss D52, solventborne gloss clear |
| Interior timber, stains and clear finishes, heavy duty solventborne gloss | 2i 4.1 | D82 | Heavy duty finish - Resene Polythane D53, solventborne gloss clear; for particleboard and fibre board - Resene Particleboard Sealer D43, waterborne sealer | Resene Polythane D53, solventborne gloss clear | Resene Polythane D53, solventborne gloss clear |
| Interior timber, stains and clear finishes, solventborne satin | 2i 4.3 | D82 | Stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or Clear finish - Resene Waterborne Colorwood Reducing Base D50a, waterborne clear (optional) | Resene Poly-Flat D52, solventborne flat clear; or For particleboard and fibre board - Resene Aquaclear D59, waterborne urethane | Resene Poly-Satin D52, solventborne satin clear |
| Interior timber, stains and clear finishes, solventborne flat | 2i 4.5 | D82 | Stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or Clear finish - Resene Waterborne Colorwood Reducing Base D50a, waterborne clear (optional) | Resene Poly-Flat D52, solventborne flat clear; or For particleboard and fibre board - Resene Aquaclear D59, waterborne urethane | Resene Poly-Flat D52, solventborne flat clear |

### Interior timber floors, stains and clear finishes dedicated section for floors

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec2_Timber_Interior_Ext.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd/4th/5th coat |
| --- | --- | --- | --- | --- | --- |
| Interior timber, stains and clear finishes, waterborne gloss | 2i 3.1 F | D82 | For stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or Clear finish - Resene Aquaclear D59, waterborne gloss urethane | Resene Aquaclear D59, waterborne gloss urethane | Resene Aquaclear D59, waterborne gloss urethane |
| Interior timber, stains and clear finishes, waterborne semi-gloss | 2i 3.2 F | D82 | For stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or Clear finish - Resene Aquaclear D59, waterborne gloss urethane | Resene Aquaclear D59, waterborne semi-gloss urethane | Resene Aquaclear D59, waterborne semi-gloss urethane |
| Interior timber, stains and clear finishes, waterborne satin | 2i 3.3 F | D82 | For stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or Clear finish - Resene Aquaclear D59, waterborne gloss urethane | Resene Aquaclear D59, waterborne satin urethane | Resene Aquaclear D59, waterborne satin urethane |
| Description: | Resene One-Line Spec: | Surface prep: | 1st coat: | 2nd coat: | 3rd/4th coat: |
| Interior timber, stains and clear finishes, solventborne gloss | 2i 4.1 F | D82 | For heavy duty finish - Resene Polythane D53, solventborne gloss clear; or For particle board and fibre board - Resene Particle Board Sealer D43, waterborne sealer | Resene Polythane D53, solventborne gloss clear | Resene Polythane D53, solventborne gloss clear |
| Interior timber, stains and clear finishes, solventborne satin | 2i 4.3 F | D82 | For stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or For clear finish - Resene HD Poly-Satin D52, solventborne satin clear; or For particle board and fibre board - Resene Aquaclear D59, waterborne urethane | Resene HD Poly-Satin D52, solventborne satin clear | Resene HD Poly-Satin D52, solventborne satin clear |

### Interior timber joinery

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec3_Timber_Joinery.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd coat |
| --- | --- | --- | --- | --- | --- |
| Interior timber joinery, waterborne gloss | 3i 1.1 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45; waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Enamacryl D309, waterborne gloss enamel | Resene Enamacryl D309, waterborne gloss enamel |
| Interior timber joinery, waterborne semi-gloss | 3i 1.2 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45; waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Lustacryl D310, waterborne semi-gloss enamel | Resene Lustacryl D310, waterborne semi-gloss enamel |
| Interior timber joinery, waterborne low sheen | 3i 1.4 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45; waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene SpaceCote Low Sheen D311, waterborne low sheen enamel | Resene SpaceCote Low Sheen D311, waterborne low sheen enamel |
| Interior timber joinery, waterborne flat | 3i 1.5 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45; waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene SpaceCote Flat D314, waterborne flat enamel | Resene SpaceCote Flat D314, waterborne flat enamel |
| Interior timber joinery, solventborne gloss | 3i 2.1 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45; waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Acrylic Undercoat D404, waterborne undercoat | Resene Super Gloss D32, solventborne gloss |
| Interior timber joinery, solventborne semi-gloss | 3i 2.2 | D82; and Resene TimberLock D48, solventborne preserver/conditioner | For normal recommended system - Resene Quick Dry D45; waterborne primer/undercoat; or For timber that stains - Resene Wood Primer D40, solventborne primer; or For painting over varnish - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Lusta-Glo D33, solventborne semi-gloss | Resene Lusta-Glo D33, solventborne semi-gloss |

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd/4th/5th coat |
| --- | --- | --- | --- | --- | --- |
| Interior timber joinery, clear waterborne gloss | 3i 3.1 | D82 | For stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or For clear finish - Resene Waterborne Colorwood Reducing Base D50a, waterborne clear (optional) | Resene Aquaclear D59, waterborne gloss urethane | Resene Aquaclear D59, waterborne gloss urethane |
| Interior timber joinery, clear waterborne semi-gloss | 3i 3.2 | D82 | For stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or For clear finish - Resene Waterborne Colorwood Reducing Base D50a, waterborne clear (optional) | Resene Aquaclear D59, waterborne semi-gloss urethane | Resene Aquaclear D59, waterborne semi-gloss urethane |
| Interior timber joinery, clear waterborne satin | 3i 3.3 | D82 | For stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or For clear finish - Resene Waterborne Colorwood Reducing Base D50a, waterborne clear (optional) | Resene Aquaclear D59, waterborne satin urethane | Resene Aquaclear D59, waterborne satin urethane (5th coat optional) |
| Interior timber joinery, clear solventborne gloss | 3i 4.1 | D82 | For stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or For clear finish - Resene Waterborne Colorwood Reducing Base D50a, waterborne clear (optional) | Resene Waterborne Colorwood D50a, waterborne wood stain | 3rd coat: Resene Poly-Flat D52 4th/5th coat: Resene Poly-Gloss D52, solventborne gloss clear |
| Interior timber joinery, clear heavy duty solventborne gloss | 3i 4.1 | D82 | For heavy duty finish - Resene Polythane D53, solventborne gloss clear; or For particle board and fibre board - Resene Particle Board Sealer D43, waterborne sealer | Resene Polythane D53, solventborne gloss clear | Resene Polythane D53, solventborne gloss clear No 5th coat required. |
| Interior timber joinery, clear solventborne satin | 3i 4.1 | D82 | For stained finish - Resene Waterborne Colorwood D50a, waterborne wood stain; or For clear finish - Resene Waterborne Colorwood Reducing Base D50a, waterborne clear (optional) | Resene Poly-Flat D52, solventborne flat clear | Resene Poly-Satin D52, solventborne satin clear No 5th coat required. |

### Interior paperfaced plaster/solid plaster/fibrous plaster

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec15_Plaster_Interior.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd/4th coat |
| --- | --- | --- | --- | --- | --- |
| Interior paperfaced plaster/solid plaster/fibrous plaster, waterborne gloss | 15i 1.1 Level 5 | D84; D85; D87; Resene Broadwall Surface Prep & Seal D807, waterborne prep | (if reqd): For wet area, stained, porous or powdery areas - Resene Sureseal D42; solventborne sealer For new wet areas - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Enamacryl D309, waterborne gloss enamel | Resene Enamacryl D309, waterborne gloss enamel |
|  | 15i 1.11 L 5 | For Level 5 Resene Broadwall 3 in 1 system - Resene One-Line Spec. No. 15i 1.11 L 5 Replace Resene Broadwall Surface Prep & Seal with Resene Broadwall 3 in 1 D810 in the clause above |
|  | 15i 1.1 L 4 | Remove Resene Broadwall Surface Prep & Seal from Surface prep and add 1st coat: Resene Broadwall Waterborne Wallboard Sealer D403, waterborne sealer |
| Interior paperfaced plaster/solid plaster/fibrous plaster, waterborne semi-gloss | 15i 1.2 Level 5 | D84; D85; D87; Resene Broadwall Surface Prep & Seal D807, waterborne prep | (if reqd): For wet area, stained, porous or powdery areas - Resene Sureseal D42; solventborne sealer For new wet areas - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Lustacryl D310, waterborne semi-gloss enamel | Resene Lustacryl D310, waterborne semi-gloss enamel |
|  | 15i 1.21 L 5 | For Level 5 Resene Broadwall 3 in 1 system - Resene One-Line Spec. No. 15i 1.21 L 5 Replace Resene Broadwall Surface Prep & Seal with Resene Broadwall 3 in 1 D810 in the clause above |
|  | 15i 1.2 L 4 | For Level 4 system - Resene One-Line Spec No. 15i 1.2 L 4 Remove Resene Broadwall Surface Prep & Seal from Surface prep and add 1st coat: Resene Broadwall Waterborne Wallboard Sealer D403, waterborne sealer |
| Interior paperfaced plaster/solid plaster/fibrous plaster, waterborne satin | 15i 1.3 Level 5 | D84; D85; D87; Resene Broadwall Surface Prep & Seal D807, waterborne prep | (if reqd): For wet area, stained, porous or powdery areas - Resene Sureseal D42; solventborne sealer | Resene Lumbersider D34, waterborne satin | Resene Lumbersider D34, waterborne satin |
|  | 15i 1.31 L 5 | For Level 5 Resene Broadwall 3 in 1 system - Resene One-Line Spec. No. 15i 1.31 L 5 Replace Resene Broadwall Surface Prep & Seal with Resene Broadwall 3 in 1 D810 in the clause above |
|  | 15i 1.3 L 4 | For Level 4 system - Resene One-Line Spec No. 15i 1.3 L 4 Remove Resene Broadwall Surface Prep & Seal from Surface prep and add 1st coat: Resene Broadwall Waterborne Wallboard Sealer D403, waterborne sealer |
| Interior paperfaced plaster/solid plaster/fibrous plaster, waterborne low sheen | 15i 1.4 ZS Level 5 | D84; D85; D87; Resene Broadwall Surface Prep & Seal D807, waterborne prep | (if reqd): For wet area, stained, porous or powdery areas - Resene Sureseal D42; solventborne sealer | Resene Zylone Sheen or Resene Zylone Sheen VOC Free D302, waterborne low sheen | Resene Zylone Sheen or Resene Zylone Sheen VOC Free D302, waterborne low sheen |
|  | 15i 1.41 ZS L 5 | For Level 5 Resene Broadwall 3 in 1 system - Resene One-Line Spec. No. 15i 1.41 ZS L 5 Replace Resene Broadwall Surface Prep & Seal with Resene Broadwall 3 in 1 D810 in the clause above |
|  | 15i 1.4 ZS L 4 | For Level 4 system - Resene One-Line Spec No. 15i 1.4 ZS L 4 Remove Resene Broadwall Surface Prep & Seal from Surface prep and add 1st coat: Resene Broadwall Waterborne Wallboard Sealer D403, waterborne sealer |
| Interior paperfaced plaster/solid plaster/fibrous plaster, waterborne low sheen enamel | 15i 1.4 SC Level 5 | D84; D85; D87; Resene Broadwall Surface Prep & Seal D807, waterborne prep | (if reqd): For wet area, stained, porous or powdery areas - Resene Sureseal D42; solventborne sealer; or For new wet areas - Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene SpaceCote Low Sheen D311, waterborne low sheen enamel | Resene SpaceCote Low Sheen D311, waterborne low sheen enamel |
|  | 15i 1.41 SC Level 5 | For Level 5 Resene Broadwall 3 in 1 system - Resene One-Line Spec. No. 15i 1.41 SC Level 5 Replace Resene Broadwall Surface Prep & Seal with Resene Broadwall 3 in 1 D810 in the clause above |
|  | 15i 1.4 SC L 4 | For Level 4 system - Resene One-Line Spec No. 15i 1.4 SC L 4 Remove Resene Broadwall Surface Prep & Seal from Surface prep and add 1st coat: Resene Broadwall Waterborne Wallboard Sealer D403, waterborne sealer |
| Interior paperfaced plaster/solid plaster/fibrous plaster, waterborne flat | 15i 1.5 Level 5 | D84; D85; D87; Resene Broadwall Surface Prep & Seal D807, waterborne prep | (if reqd): For wet area, stained, porous or powdery areas - Resene Sureseal D42; solventborne sealer | Resene Zylone 20 D37, waterborne flat | Resene Zylone 20 D37, waterborne flat |
|  | 15i 1.51 L 5 | For Level 5 Resene Broadwall 3 in 1 system - Resene One-Line Spec. No. 15i 1.51 L 5 Replace Resene Broadwall Surface Prep & Seal with Resene Broadwall 3 in 1 D810 in the clause above |
|  | 15i 1.5 L 4 | For Level 4 system - Resene One-Line Spec No. 15i 1.5 L 4 Remove Resene Broadwall Surface Prep & Seal from Surface prep and add 1st coat: Resene Broadwall Waterborne Wallboard Sealer D403, waterborne sealer |
| Interior paperfaced plaster/solid plaster/fibrous plaster, waterborne flat - ceiling | 15i 1.5 Level 5 Ceiling | D84; D85; D87; Resene Broadwall Surface Prep & Seal D807, waterborne prep | (if reqd): For wet area, stained, porous or powdery areas - Resene Sureseal D42; solventborne sealer | Resene Ceiling Paint D305, waterborne flat | Resene Ceiling Paint D305, waterborne flat |
|  | 15i 1.51 Level 5 Ceiling | For Level 5 Resene Broadwall 3 in 1 system - Resene One-Line Spec. No. 15i 1.51 Level 5 Ceiling Replace Resene Broadwall Surface Prep & Seal with Resene Broadwall 3 in 1 D810 in the clause above |
|  | 15i 1.5 L 4 Ceiling | For Level 4 system - Resene One-Line Spec No. 15i 1.5 L 4 Ceiling Remove Resene Broadwall Surface Prep & Seal from Surface prep and add 1st coat: Resene Broadwall Waterborne Wallboard Sealer D403, waterborne sealer |
| Interior paperfaced plaster/solid plaster/fibrous plaster, waterborne flat | 15i 1.5 SC Level 5 | D84; D85; D87; Resene Broadwall Surface Prep & Seal D807, waterborne prep | (if reqd): For wet area, stained, porous or powdery area, Resene Sureseal D42, solventborne sealer; or For new wet area, Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene SpaceCote Flat D314, waterborne flat enamel | Resene SpaceCote Flat D314, waterborne flat enamel |
|  | 15i 1.51 SC L 5 | For Level 5 Resene Broadwall 3 in 1 system - Resene One-Line Spec. No. 15i 1.51 SC L 5 Replace Resene Broadwall Surface Prep & Seal with Resene Broadwall 3 in 1 D810 in the clause above |
|  | 15i 1.5 SC L 4 | For Level 4 system - Resene One-Line Spec No. 15i 1.5 SC L 4 Remove Resene Broadwall Surface Prep & Seal from Surface prep and add 1st coat: Resene Broadwall Waterborne Wallboard Sealer D403, waterborne sealer |
| Interior paperfaced plaster/solid plaster/fibrous plaster, solventborne gloss | 15i 2.1 Level 5 | D84; D85; D87; Resene Broadwall Surface Prep & Seal D807, waterborne prep | Resene Sureseal D42, solventborne sealer; or For new wet areas, Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Acrylic Undercoat D404, waterborne undercoat | Resene Super Gloss D32, solventborne gloss |
|  | 15i 1.21 L 5 | For Level 5 Resene Broadwall 3 in 1 system - Resene One-Line Spec. No. 15i 1.21 L 5 Replace Resene Broadwall Surface Prep & Seal with Resene Broadwall 3 in 1 D810 in the clause above |
|  | 15i 2.1 Level 4 | For Level 4 system - Resene One-Line Spec No. 15i 2.1 Level 4 Remove Resene Broadwall Surface Prep & Seal from Surface prep and add 1st coat: Resene Broadwall Waterborne Wallboard Sealer D403, waterborne sealer |
| Interior paperfaced plaster/solid plaster/fibrous plaster, solventborne semi-gloss | 15i 2.2 Level 4 | D84; D85; D87; Resene Broadwall Surface Prep & Seal D807, waterborne prep | Resene Sureseal D42, solventborne sealer; or For new wet areas, Resene Waterborne Smooth Surface Sealer D47a, waterborne sealer | Resene Lusta-Glo D33, solventborne semi-gloss | Resene Lusta-Glo D33, solventborne semi-gloss |
|  | 15i 2.21 L 5 | For Level 5 Resene Broadwall 3 in 1 system - Resene One-Line Spec. No. 15i 2.21 L 5 Replace Resene Broadwall Surface Prep & Seal with Resene Broadwall 3 in 1 D810 in the clause above |
|  | 15i 2.2 Level 4 | For Level 4 system - Resene One-Line Spec No. 15i 2.2 Level 4, Remove Resene Broadwall Surface Prep & Seal from Surface prep and add 1st coat: Resene Broadwall Waterborne Wallboard Sealer D403, waterborne sealer |

### Interior metallic finishes

For more information: Refer to Resene website

http://www.resene.co.nz/archspec/datashts/spec25_Special_Effects.pdf

| Description | Resene One-Line Spec | Surface prep | 1st coat | 2nd coat | 3rd/4th coat |
| --- | --- | --- | --- | --- | --- |
| Interior metallic finishes, waterborne metallic finish on Anaglypta, Scandatex, etc | 25i 1.3/5 | D84; D85 | Resene Broadwall Waterborne Wallboard Sealer D403, waterborne sealer | Resene Lumbersider D34, waterborne satin | Resene Enamacryl Metallic D309a, waterborne metallic 5th coat: Resene Aquaclear D59, waterborne gloss urethane (optional) |
| Interior metallic finishes, waterborne metallic finish on paperfaced plasterboard | 25i 1.3/51 | D84; D85 | Resene Broadwall Surface Prep and Seal D807, waterborne surfacer/sealer or Resene Broadwall 3 in 1 Sealer D810, waterborne surfacer/sealer | Resene Lumbersider D34, waterborne satin | Resene Enamacryl Metallic D309a, waterborne metallic 5th coat: Resene Aquaclear D59, waterborne gloss urethane (optional) |
| Interior metallic finishes, waterborne metallic finish on MDF joinery/doors | 25i 1.3/52 | D82 | Resene Quick Dry D45, waterborne primer/undercoat | Resene Lumbersider D34, waterborne satin | Resene Enamacryl Metallic D309a, waterborne metallic 5th coat: Resene Aquaclear D59, waterborne gloss urethane (optional) |
| Interior metallic finishes, waterborne pearlescent finish on interior surfaces | 25i 1.3/52 P | D82 for MDF; D84/D85 | Normal recommended system: Resene Quick Dry D45, waterborne primer/undercoat; or For paperfaced plasterboard Resene Broadwall Surface Prep and Seal D807, waterborne surfacer/sealer or Resene Broadwall 3 in 1 Sealer D810, waterborne surfacer/sealer | Resene Lumbersider D34, waterborne satin | 3rd coat: Resene Lumbersider D34, waterborne satin 4th coat: Resene Pearl Shimmer D312, waterborne pearlescent 5th coat: Resene Aquaclear D59, waterborne gloss urethane (optional) |
| Interior metallic finishes, solventborne metallic finish on concrete floor | 25i 2.3/5 | D83 | Resene Armourcote 510 RA40, high solids epoxy | Resene Imperite I.F. 503 RA81, solventborne metallic | Resene Uracryl 400 Series Clear, solventborne clear |
| Interior metallic finishes, solventborne metallic finish on MDF Joinery/doors | 25i 2.3/51 | D82 | Refer Resene Paints Ltd | Resene Imperite I.F. 503 RA81, solventborne metallic | Resene Imperite I.F. 502 Clear RA82, semi-gloss clear |

### Other Resene interior systems

6i INTERIOR FERROUS METALS

Refer to http://www.resene.co.nz/archspec/datashts/spec6_Ferrous_Metals.pdf

7i INTERIOR NON-FERROUS METALS

Refer to http://www.resene.co.nz/archspec/datashts/spec7_Non-Ferrous_Metals.pdf

9i INTERIOR TOTARA AND MATAI TIMBER ONLY

Refer to http://www.resene.co.nz/archspec/datashts/spec9_Matai_Totara.pdf

11i INTERIOR GLASS, GLAZED TILES, FORMICA, POLYETHYLENE, POLYPROPYLENE AND BAKED ENAMEL SYSTEMS

Refer to http://www.resene.co.nz/archspec/datashts/spec11_Enamel_Glass_Tiles.pdf

12i INTERIOR GLASS REINFORCED POLYESTER, GLASS REINFORCED EPOXY, PVC, ACRYLIC SHEETING

Refer to http://www.resene.co.nz/archspec/datashts/spec12_Plastic_Materials.pdf

13i INTERIOR BRICK AND TERRACOTTA, CLEAR FINISHES

Refer to http://www.resene.co.nz/archspec/datashts/spec13_Brick_Terracotta.pdf

14i INTERIOR CLEAR FINISHES ON CLAY TILES, ABSORBENT TILES, STONE AND SLATE, DECORATIVE AGGREGATE FLOORING

Refer to http://www.resene.co.nz/archspec/datashts/spec14_Clay_Tiles_Stone.pdf

16i CANVAS, SCANDATEX AND HESSIAN

Refer to http://www.resene.co.nz/archspec/datashts/spec16_Canvas_Wallpaper.pdf

18i SPECIALIST FLOORING SYSTEMS

Refer to http://www.resene.co.nz/archspec/datashts/spec18_Flooring_Specialist.pdf

19i ANTI GRAFFITI SYSTEMS

Refer to http://www.resene.co.nz/archspec/datashts/spec19_Anti-Graffiti_System.pdf

20i TEXTURED COATINGS

Refer to http://www.resene.co.nz/archspec/datashts/spec20_Textured_Coatings.pdf

21i PAINT EFFECTS

Refer to http://www.resene.co.nz/archspec/datashts/spec21_Paint_Effects.pdf

26i SPECIALIST INTERIOR FINISHES: RESENE ARMOURCAT ACID-CATALYSED

Refer to http://www.resene.co.nz/archspec/datashts/spec26_Specialist_Acid_Cat.pdf

REFERENCED DOCUMENTS

The following documents are incorporated into this worksection by reference:

---AS/NZS 2310	2002	Glossary of paint and painting terms

--AS/NZS 2311	2000	Guide to the painting of buildings

----AS 3750		Paints for steel structures

--AS/NZS 3750.9	1994	Organic zinc-rich primer

NATSPEC TECHreport	 	Specifying ESD

SUSDP	2008	Standard for the Uniform Scheduling of Drugs and Poisons No. 23, Appendix I - Uniform Paint Standard, Australian Health Minister's Advisory Council for National Drugs and Poisons Schedule Committee